## Slide 1: Compaction

## Slide 2: 1.1 Methods for Soil Improvement
Ground
Reinforcement
Ground
Improvement
Ground
Treatment
Stone Columns
Soil Nails
Deep Soil Nailing
Micropiles (Mini-piles)
Jet Grouting
Ground Anchors
Geosynthetics
Fiber Reinforcement
Lime Columns
Vibro-Concrete Column
Mechanically Stabilized Earth
Biotechnical
Deep Dynamic Compaction
Drainage/Surcharge
Electro-osmosis
Compaction grouting
Blasting
Surface Compaction
Soil Cement
Lime Admixtures
Flyash
Dewatering
Heating/Freezing
Vitrification
Compaction
Shaefer, 1997

## Slide 3: 1.1 Methods for Soil Improvement- Jet Grouting
Courtesy of Menard-soltraitement

## Slide 4: 1.1 Methods for Soil Improvement-Soil Nailing
Courtesy of Atlas Copco Rock Drilling Equipment

## Slide 5: 1.2 Elephant and Compaction
Heavy Weight
Question?
The compaction result is not good. Why?
He He! I’m smart.

## Slide 6: 2. Compaction

## Slide 7: Compaction and Objectives
Many types of earth construction, such as roads, dams, retaining walls, highways, and airport, require man-placed soil, or fill. To compact a soil, that is, to place it in a dense state.
The dense state is achieved through the reduction of the air voids in the soil, with little or no reduction in the water content.
This process must not be confused with consolidation, in which water is squeezed out under the action of a continuous static load.
Objectives:
Increase shear strength
Decrease permeability
Decrease future settlements

## Slide 8: Compaction
Soil compaction is defined as the method of mechanically increasing the density of soil. In construction, this is a significant part of the building process. If performed improperly, settlement of the soil could occur and result in unnecessary maintenance costs or structure failure

## Slide 9: Compaction: Laboratory Tests
BASIC THEORY
Developed by R.R. Proctor at 1920-an with 4 variables :
  Compaction efforts (Compaction Energy)
  Soil types
  Water content
  Dry Unit Weight
LABORATORY COMPACTION TEST
  Standard Proctor Test
  Modified Proctor Test

## Slide 10: STANDARD PROCTOR TEST
The soil is compacted in cylindrical mold
Specification of test and equipment
  Hammer weight = 2,5 kg (5,5 lb)
  Falling height = 0.3 m (1 ft)
  Number of layers = 3
  No. of blows/layer = 25
  Mold size: 945 cc (1/30 ft3 )
  Compaction effort = 595 kJ/m3
  Soil type = pass sieve no. 4
The test is carried out several time with different water contents
After compacted, the weight, moisture content and unit weight of samples are measured
Test Standard :
  AASHTO T 99
  ASTM D698

## Slide 11: MODIFIED PROCTOR TEST
The soil is compacted at cylindrical tube
Specification of test and equipments
  Hammer weight = 4.5 kg (10 lb)
  Falling height = 0.457m (1.5 ft)
  Number of layers = 5
  No. of blows/layer = 25
  Compaction effort = 2693 kJ/m3
  Soil type = pass sieve no. 4
The test is carried out several time with different water content
After compacted, the weight, moisture content and unit weight of samples are measured
Test Standard :
  AASHTO T 180
  ASTM D1557
Compaction effort:
4.5 x Standard Proctor

## Slide 12: Results-Explanation
w
d
(wopt, d max)
Below wopt (dry side of optimum):
As the water content increases, the particles develop larger and larger water films around them, which tend to “lubricate” the particles and make them easier to be moved about and reoriented into a denser configuration.
At wopt:
The density is at the maximum, and it does not increase any further.
Above wopt (wet side of optimum):
The energy applied is mainly transferred to water phase and not soil skeleton. Water starts to replace soil particles in the mold, and since w << s the dry density starts to decrease.
Lubrication or loss of suction??

## Slide 13: Results-Explanation
Swelling of compacted clays is greater for those compacted dry of optimum. They have a relatively greater deficiency of water and therefore have a greater tendency to adsorb water and thus swell more.
w
d
(wopt, d max)
Higher swelling potential
Higher shrinkage potential

## Slide 15: Results-Explanation
Zero air void
Water content w (%)
Dry density d (Mg/m3)
Dry density d (lb/ft3)
Line of optimums
Modified Proctor
Standard Proctor
Peak point
Line of optimum
Zero air void
d max
wopt
Notes: Optimum water content is typically slightly less than the plastic limit.

## Slide 16: Structure of Compacted Clays
For a given compactive effort the soil tends to be more flocculated (random) for compaction on the dry side as compared on the wet side.
For a given molding water content, increasing the compactive effort tends to disperse (parallel oriented) the soil.

## Slide 17: Engineering Properties: Permeability

## Slide 18: Engineering Properties: Summary
Dry side
Wet side
Permeability
Compressibility
Swelling
Strength
Structure
More random
More oriented (parallel)
More permeable
More compressible in high pressure range
More compressible in low pressure range
Swell more, higher water deficiency
Higher
*Shrink more

## Slide 19
4 types of compaction effort on soil :
  Pressure
  Vibration
  Kneading
  Impact

## Slide 20: Field Compaction: Equipment
Smooth-wheel roller (drum)
100% coverage under the wheel
Contact pressure up to 380 kPa
Can be used on all soil types except for rocky soils.
Compactive effort: static weight
The most common use of large smooth wheel rollers is for proof-rolling subgrades and compacting asphalt pavement.
`

## Slide 21: Field Compaction: Equipment
Pneumatic (or rubber-tired) roller
80% coverage under the wheel
Contact pressure up to 700 kPa
Can be used for both granular and fine-grained soils.
Compactive effort: static weight and kneading.
Can be used for highway fills or earth dam construction.

## Slide 22: Field Compaction: Equipment
Sheepsfoot rollers
Has many round or rectangular shaped protrusions or “feet” attached to a steel drum
8% ~ 12 % coverage
Contact pressure is from 1400 to 7000 kPa
It is best suited for clayed soils.
Compactive effort: static weight and kneading.

## Slide 23: Field Compaction: Equipment
Tamping foot roller
About 40% coverage
Contact pressure is from 1400 to 8400 kPa
It is best for compacting fine-grained soils (silt and clay).
Compactive effort: static weight and kneading.

## Slide 24: Field Compaction: Equipment
Mesh (or grid pattern) roller
50% coverage
Contact pressure is from 1400 to 6200 kPa
It is ideally suited for compacting rocky soils, gravels, and sands. With high towing speed, the material is vibrated, crushed, and impacted.
Compactive effort: static weight and vibration.

## Slide 25: Field Compaction: Equipment
Vibrating drum on smooth-wheel roller
Vertical vibrator attached to smooth wheel rollers.
The best explanation of why roller vibration causes densification of granular soils is that particle rearrangement occurs due to cyclic deformation of the soil produced by the oscillations of the roller.
Compactive effort: static weight and vibration.
Suitable for granular soils

## Slide 26: Field Compaction: Equipment
  Vibrating Plate :
  Compaction equipment, which has plate shape. Sometimes called as “stamper”. Usually used for narrow area

## Slide 28
Field Compaction: Equipment
Deep Compaction

## Slide 29: Field Compaction: Equipment

## Slide 30
Characteristic of compaction equipment
  Weight and size
  Operation frequency and frequency range
Soil Characteristic
  Initial density
  Soil type
  Size and shape of soil particle
  Moisture Content
Compaction Procedure
  No. of passes of the roller
  Layer thickness
  Frequency of operation of vibrator
  Towing speed
Field Compaction: Equipment-CONDITIONER FACTORS

## Slide 31: Field Tests: Destructive Methods
Holtz and Kovacs, 1981
Methods
(a) Sand cone
(b) Balloon
(c) Oil (or water) method
Calculations
Know Ms and Vt
Get d field and w (water content)
Compare d field with d max-lab and calculate relative compaction R.C.
(a)
(b)
(c)

## Slide 32: Field Tests: Non-Destructive Methods
Holtz and Kovacs, 1981
Nuclear density meter
(a) Direct transmission
(b) Backscatter
(c) Air gap
(a)
(b)
(c)
Principles
Density
The Gamma radiation is scattered by the soil particles and the amount of scatter is proportional to the total density of the material. The Gamma radiation is typically provided by the radium or a radioactive isotope of cesium.
Water content
The water content can be determined based on the neutron scatter by hydrogen atoms. Typical neutron sources are americium-beryllium isotopes.

## Slide 33: SPECIFICATION FOR COMPACTION
End Product Specification:
Relative Compaction:
Method of Specification
  Minimum soil sample 100 kg
  Need special experience to find out the optimum moisture content in order to get optimum compaction performance

## Slide 34: HW#3 Compaction
1. The in-situ dry density of a sand is 1.72 Mg/m3. The maximum and minimum dry densities, determined by standard laboratory tests, are 1.81 and 1.54 Mg/m3, respectively. Determine the relative density of the sand.
2. An embankment for a highway 30m wide and 1.5 m in compacted thickness is to be constructed from a sandy soil trucked from a borrow pit. The water content of the sandy soil in the borrow pit is 15% and its void ratio is 0.69. The swell index is 1.2. The specification requires the embankment to be compacted to a dry unit weight of 18 kN/m3. Determine, for a 1-km length of embankment, the following:
(a)The weight of sandy soil from the borrow pit required to construct the embankment. (b) The number of truckloads of sandy soil required for the construction. The full capacity of each truck is 22.2 m3, and local government regulations require a maximum loaded capacity of 90%. (c) The weight of water per truckload of sandy soil. (d) The degree of saturation of the sandy soil in situ.

## Slide 35: HW#3 Compaction
3. A soil at a mining site is classified according to USCS as GW-GM. (a) Would this soil be suitable for the base course of a road?
(b) What type of field compaction equipment would you recommend? (c) How would you check that the desired compaction is achieved in the field? (d) Would you specify compaction dry or wet of optimum? Why?
4. The natural water content of a borrow material is known to be 105. Assuming 6000 g of wet soil is used for laboratory compaction test points, compute how much water is to be added to other 6000 g samples to bring their water contents up to 13, 17, 20, 24, and 28%.

## Slide 36
HW#3 Compaction
5. You are checking a field compacted layer of soil. The laboratory control curve has the following values.
The specification for compaction states that the compacted field soil must be at least 95% of the maximum control density and within ±2% of the optimum moisture for the control curve. You dig a hole of in the compacted layer and extract a sample that weighs 4 Ib wet and 3.4 Ib dry.
(a) What is the compacted ? The compaction water content w? The percent compaction? Does the sample meet the specification?
(b) If the density of solids is 2.7 Mg/m3. What is the compacted degree of saturation? If the sample were saturated at constant density, what would be the water content?
Water content (%) | 14 | 16 | 18 | 20 | 22 | 24
Dry unit weight , | 104 | 105.5 | 106 | 105 | 103.5 | 101
Water content (%) | 14 | 16 | 18 | 20 | 22 | 24
 | 104 | 105.5 | 106 | 105 | 103.5 | 101